## Slide 1
FLUID | COMPONENT | DESIGN CODE | MATERIAL | INSULATED (Y/N) | OP. PARAMETER | CURRENT RISK RATING | Corrosion Group : Damage Mechanism Susceptible: Internal Shell Side Cooling Water Corrosion Internal Tube Side Sulfuric Acid Corrosion External Shell Side General Corrosion External Tube Side CUI-CLSCC
TYPE | SPEC | GR | T (֯C) | P (Mpa)
 | Top Channel (Tube Side) | ASME VII DIV 1 | SS |  |  |  |  |  | LOW
 | Shell | ASME VIII DIV 1 | SS |  |  |  |  | 
 | Bottom Channel (Tube Side) | ASME VIII DIV 1 | SS |  |  |  |  | 
INSPECTION METHOD | INSPECTION COVERAGE | DAMAGE MECHANISM
UTTM | 100% of TML Location – Refer TML as per Attachment 1 | General Corrosion Sulfuric Acid Corrosion
VISUAL INSPECTION | 100% external visual inspection prior to insulation removal Ref: 1. General VI. Ext Inspection Checklist 2. CUI-CLSCC inspection checklist. And For suspected area where accessible: > 5% DPT or Eddy Current Testing with UT follow up of all relevant indication. | General Corrosion CUI-CLSCC
DPI (High Temp) | For suspected area where accessible: > 5% DPT or Eddy Current Testing with UT follow up of all relevant indication as per Attachment 2 | CUI-CLSCC