## Slide 1
FLUID | COMPONENT | DESIGN CODE | MATERIAL | INSULATED (Y/N) | OP. PARAMETER | CURRENT RISK RATING | Corrosion Group : Damage Mechanism Susceptible: Internal Steam Condensate Corrosion External Corrosion Under Insulation(CUI)
TYPE | SPEC | GR | T (֯C) | P (Mpa)
 | Head | ASME VII DIV 1 | CS |  |  |  |  |  | LOW
 | Shell | ASME VIII DIV 1 | CS |  |  |  |  | 
INSPECTION METHOD | INSPECTION COVERAGE | DAMAGE MECHANISM
UTTM (Correction Factor) | 100% of TML Location – Refer TML as per Attachment 1 | General Corrosion
VISUAL INSPECTION | External Visual Inspection (100% Coverage) And Remove >5% of suspected area (as per Attachment 2). And Follow up by UT, RT or pit gauges as required if visual inspection reveal CUI as necessary | CUI